## Slide 1: High Resolution Polar Kerr Effect Studies of CsV3Sb5
Mar, 8, 2023
David Saykin
APS March Meeting 2023
M58:11. GMAG: Light Matter Interaction
Saykin et al., arXiv: 2209.10570

## Slide 2: Collaboration
David Saykin
Erik Kountz
Aharon Kapitulnik
Dong Chen
Chandra Shenkar
Claudia Felser
Camron Farhang
Jing Xia
Brenden Ortiz
Stephen Wilson
Ronny Thomale
1 mm
1 mm

## Slide 3: Properties of CsV3Sb5
Layered Kagome metal
Superconducts below Tc = 2.5 K
Charge-density wave at Tcdw = 94 K
Ortiz et al., PRL 125, 247002 (2020)
Cs
Sb
V

## Slide 4: CDW structure in CsV3Sb5
SoD
TrH
TrH
TrH
SoD
F27.8 Mallayya et al,
arXiv: 2211.16602
Ortiz et al., PRX 11, 041030 (2021)

## Slide 5: Hints of TRSB in CsV3Sb5
Rotation of polarization at finite incidence angle
  Wu et al., Phys. Rev. B 106, 205109
  Xu et al., nphys 18,1470 (2022)
Anomalous Hall Effect
  Yu et al., PRB 104, L041103 (2021)
Magnetochiral transport at T* = 35 K
  C. Guo et al., Nature 611, 461 (2022)
uSR rate change at T* = 30 K and TCDW = 94 K
  L. Yu et al., arXiv: 2107.10714
  Khasanov et al., PRR 4, 023244
Q: Is there a time-reversal symmetry breaking?
A: Let’s test it with Polar Kerr Effect

## Slide 6: Optical properties of CsV3Sb5
Zhou et al. PRB 104, L041101 (2021)
Saykin et al., arXiv: 2209.10570
Reflectivity and Linear Birefringence

## Slide 7: Zero-Area Sagnac Interferometer
SrRuO3
Properties:
Reciprocity
Robust against:
  Linear birefringence
  Optical activity
1
Sample
Fiber
1
1
2
2
2
1
2
Xia et al., APL 89, 062508 (2006)
1550 nm
P = 100 uW
D = 27 um

## Slide 8: Diamagnetic Kerr response.
In-field Kerr signal demonstrates diamagnetic-like response onsetting at Tcdw
Zero-field Kerr signal shows no TRSB (within resolution ~30 nrad)
Saykin et al., arXiv: 2209.10570
Sample 2 (Irvine, UCSB)
Sample 1 (Stanford, Dresden)
Htrain
B
T
Data acquisition
B
T
TCDW = 93.5 K
Tbase = 4.2 K
Data acquisition
NO TRSB

## Slide 9: Summary
Studied two independently grown CsV3Sb5 samples in two different laboratories in temperature range 4.2 K < T < 300 K
We detect CDW via birefringence
We observe diamagnetic shift in Kerr signal at TCDW (in field)
We detect no spontaneous, uniform Time-Reversal Symmery Breaking within the resolution of our apparatus ~30 nanorad
    Finite-q TRSB is a possibility, but AFM order would not show diamagnetism
Saykin et al., arXiv: 2209.10570

## Slide 10: Resistance data
Saykin et al., arXiv: 2209.10570
Sample 1

## Slide 11: Kerr microscopy (Sample 2)
Finite-q TRSB (antiferromagnetic order) would not be detected by Sagnac interferometer due to finitebeam spot size ~20 um.
We see no spatial dependence of Kerr signal in 2D scan performed with 20 um resolution
Saykin et al., arXiv: 2209.10570

## Slide 12: Superconductivity in CsV3Sb5
Ortiz et al., PRL 125, 247002 (2020)

## Slide 13: Anomalous Hall Effect
Yu et al., PRB 104, L041103 (2021)

## Slide 14: Optical properties of CsV3Sb5

## Slide 15: Reflectivity and linear birefringence
We are able to detect onset of linear birefringence simultaneously with Kerr effect measurements
Saykin et al., arXiv: 2209.10570

## Slide 16: Linear Kerr effect measurements
Xu et al., nphys 18, pages 1470–1475 (2022)
Wu et al., Phys. Rev. B 106, 205109

## Slide 17: Acknowledgements
Work at Stanford University was supported by the U.S. Department of Energy,
Office of Science, Basic Energy Sciences, Division of Materials Sciences and Engineering,
under Contract DE-AC02-76SF00515.
Work at UC Irvine was supported by the Gordon and Betty Moore Foundation through Grant GBMF10276.
S.D.W. and B.R.O. acknowledge support via the UC Santa Barbara NSF Quantum Foundry funded via the Q-AMASE-i pro- gram under award DMR-1906325.
R.T. acknowledges support from the Deutsche Forschungsgemeinschaft (DFG, German Research Foundation) through QUAST FOR 5249-449872909 (Project P3), through Project-ID 258499086-SFB 1170, and from the Würzburg-Dresden Cluster of Excellence on Complexity and Topology in Quantum Matter –
ct.qmat Project-ID 390858490-EXC 2147.