## Slide 1: Polar Kerr Effect Studies of Kagome Metals CsV3Sb5 and ScV6Sn6
March 7, 2024
David Saykin
APS March Meeting 2024
W16: Competing Orders in the Kagome Lattice Superconductors
Saykin et al., PRL 131, 016901 (2023)
Notes: Samples came from MPI Dresden,
Work was funded by DOE, Office of Science, Basic Energy Sciences, Division of Materials Sciences and Engineering, under Contract DE-AC02-76SF00515.
This presentation is continuation of results published in PRL and concentrates on new results.

## Slide 2: Part 1. Introduction Part 2. Kerr effect measurements
W16: D. Saykin

## Slide 3: CsV3Sb5 and ScV6Sn6
Layered Kagome metals with Charge-density wave at Tcdw ~ 94 K
Ortiz et al., PRL 125, 247002 (2020)
Arachchige et al., PRL 129, 216402 (2022)
Cs
Sb
V
Sc
V
Sn1
Sn2
Sn3
92 K
92 K
Notes: d-electrons of vanadium contribute to bands near fermi-energy

## Slide 4: TRSB at CDW?
“Anomalous” Hall Effect
uSR rate change at TCDW
Yu et al., PRB 104, L041103 (2021)
Yi, PRB 109, 035124 (2024)
Khasanov et al., PRR 4, 023244 (2022)
Guguchia et al., arXiv:2304.06436
CsV3Sb5
ScV6Sn6
Notes: Add optical measurement here. Liang Wu.
Say “TRSB associated with CDW”

## Slide 5: TRSB at CDW?
Wu et al., PRB 106, 205109
Xu et al., nphys 18, 1470–1475 (2022)
Farhang et al., ncomms 14, 5326 (2023)
1550 nm vs 800 nm
CsV3Sb5
Notes: Add optical measurement here. Liang Wu.
TRSB associated with CDW

## Slide 6: Optical properties of CsV3Sb5
5000
Wavelength (nm)
1000
1550
800 nm
800
Zhou et al. PRB 104, L041101 (2021)
1550 nm vs 800 nm
Notes: Add optical measurement here. Liang Wu.
TRSB associated with CDW

## Slide 7: Part 1. Introduction Part 2. Kerr effect measurements
W16: D. Saykin

## Slide 8: Zero-Area Sagnac Interferometer
Reciprocal by design
Robust against optical activity:
  Linear birefringence
  Circular dichroism
  Chiral crystal stacking
  …
Sample
Fiber
1
2
Xia et al., APL 89, 062508 (2006)
P = 100 uW
D = 25 um
Notes: Remove “1” and “2”.
Talk about SRO faster.
Add labels "(b) no field", "(c) field train"

## Slide 9: MOKE in SrRuO3
SrRuO3
Xia et al., APL 89, 062508 (2006)
No field
training
Field
trained
25
Notes: Say that sign of MOKE changes with the sign of the training field.

## Slide 10
In-field Kerr signal demonstrates diamagnetic-like response onsetting at Tcdw
Zero-field Kerr signal shows no TRSB (within resolution ~30 nrad)
Saykin et al., PRL 131, 016901 (2023)
Sample 2 (Irvine, UCSB)
Sample 1 (Stanford, Dresden)
Htrain
B
T
Data acquisition
B
T
TCDW = 93.5 K
Tbase = 4.2 K
Data acquisition
CsV3Sb5 @
1550 nm
Notes: Remove Camron's data. Just add text to mention.

## Slide 11: ScV6Sn6 @
In-field Kerr signal demonstrates diamagnetic-like response onsetting at Tcdw
Zero-field Kerr signal shows no TRSB (within resolution ~50 nrad)
CsV3Sb5 @
1550 nm
1550 nm
Notes: Remove Camron's data. Just add text to mention.

## Slide 12: ScV6Sn6 @
CsV3Sb5 @
830 nm
830 nm

## Slide 13: Summary
Studied CsV3Sb5 and ScV6Sn6 at 1550 and 830 nm
We observe shift in Kerr signal at TCDW in finite magnetic field at 1550 nm, but not at 830 nm
We detect no spontaneous (uniform) Time-Reversal Symmetry Breaking
Saykin et al., PRL 131, 016901 (2023)
CsV3Sb5 @
1550 nm
ScV6Sn6 @
1550 nm
Notes: Label plot "CVS @ 1550"
Less text

## Slide 14: Part 1. Introduction Part 2. Kerr effect measurements Appendix
W16: D. Saykin

## Slide 15: Oppeneer, Theory of the Magneto-Optical Kerr Effect in Ferromagnetic Compounds

## Slide 16: Optical properties of CsV3Sb5
Zhou et al. PRB 104, L041101 (2021)
Hu et al., PRB 107, 165119 (2023)
ScV6Sn6
5000
Wavelength (nm)
1000
1550
830 nm
830
CsV3Sb5
Notes: Lorenz transition in the regime of our probing laser was shown to be associated with CDW.
Label vertical lines (instead of photon energy)

## Slide 17: Optical properties of CsV3Sb5

## Slide 18: Reflectivity and linear birefringence
We are able to detect onset of linear birefringence simultaneously with Kerr effect measurements
Saykin et al., arXiv: 2209.10570

## Slide 19: Resistance data
Saykin et al., arXiv: 2209.10570
Sample 1

## Slide 20: Anomalous Hall Effect
Yu et al., PRB 104, L041103 (2021)

## Slide 21: Superconductivity in CsV3Sb5
Ortiz et al., PRL 125, 247002 (2020)

## Slide 22: Chiral Flux phase
Theoretical predictions of Chiral flux state:
  Feng et al. PRB 104, 165136 (2021)
  Lin et al. PRB 104, 045122 (2021)
  Park et al. PRB 104, 035142 (2021)

## Slide 23: CDW structure in CsV3Sb5
SoD
TrH
TrH
TrH
SoD
Ortiz et al., PRX 11, 041030 (2021)

## Slide 24: Kerr microscopy (Sample 2)
Finite-q TRSB (antiferromagnetic order) would not be detected by Sagnac interferometer due to finite beam spot size ~20 um.
We see no spatial dependence of Kerr signal in 2D scan performed with 20 um resolution
Saykin et al., arXiv: 2209.10570

## Slide 25: ScV6Sn6 @
Reflectivity and Birefringence
(each line is shifted)
Kerr effect
1550 nm

## Slide 26
Reflectivity and Birefringence
Kerr effect
CsV3Sb5 @
830 nm

## Slide 27: ScV6Sn6 @
Reflectivity and Birefringence
(each line is shifted)
Kerr effect
830 nm
Notes: Make pictures for 1550 and 830 to make it easy to see which length is discussed

## Slide 28: Acknowledgements
Work at Stanford University was supported by the U.S. Department of Energy,
Office of Science, Basic Energy Sciences, Division of Materials Sciences and Engineering,
under Contract DE-AC02-76SF00515.
Work at UC Irvine was supported by the Gordon and Betty Moore Foundation through Grant GBMF10276.
S.D.W. and B.R.O. acknowledge support via the UC Santa Barbara NSF Quantum Foundry funded via the Q-AMASE-i pro- gram under award DMR-1906325.
R.T. acknowledges support from the Deutsche Forschungsgemeinschaft (DFG, German Research Foundation) through QUAST FOR 5249-449872909 (Project P3), through Project-ID 258499086-SFB 1170, and from the Würzburg-Dresden Cluster of Excellence on Complexity and Topology in Quantum Matter –
ct.qmat Project-ID 390858490-EXC 2147.